Description:   VIT-1075 is compounded with 100% FKM base polymer. This product is

compounded to ensure performance sealing.  VIT-1075 does not contain

any regrind or reprocessed FKM which can reduce a product’s

physical properties. VIT-1075 is compounded by an independent licensed

Chemours® custom rubber mixer.

Product Type:  “A”                             		  Fluorine: 66%

ASTM: D2000M5HK710A1-10B38Z1

Z1=75 Shore A

Not recommended for:  service in acids, steam, hot water, low molecular weight esters & ketones, certain amines, hot anhydrous hydrofluoric or chlosulphonic acids and alkyl phosphate esters.

Typical Physical Properties

| Durometer (Shore A) Hardness | 75 +/-5 |
| --- | --- |
| Tensile Strength (psi) | 1200 |
| Elongation at Break (%) | 250 |
| Modulus at 100% Elongation (psi) | 450 |
| Specific Gravity | 1.89 |
| Temperature Rating (operating) | -20°F to +400°F |
| Color | Black |

*Physical properties shown were obtained on a molded .080” thick ASTM sample

These properties are typical results, and should not be used to set quality control specifications.

Proudly Manufactured in the USA

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391