VIT-1275 - BLUE

Proudly manufactured in the USA

Description: Blue General Purpose Fluoroelastomer (Viton)  It is formulated  with 100% virgin fluoroelastomer.

Not recommended for:  service in acids, steam and hot water, low molecular weight esters & ketones, certain amines, hot anhydrous hydrofluoric or chlosulphonic acids and alkyl phosphate esters.

Typical Physical Properties

| Durometer (Shore A) Hardness | 75+/-5 |
| --- | --- |
| Tensile Strength (psi) | 1200 |
| Elongation | 200% |
| Temperature Rating (operating) | -20(F to +400(F |
| Color | Blue |
| Specific Gravity | 2.0 |
| Finish | Smooth with light talc |

Physical Properties shown were obtained on a molded .080” ASTM Sample.   These are typical results.

It is the customers responsibility to qualify this product for its fitness for use.  This product is NOT recommended for mineral acids, ketones, low molecular weight esters or nitro hydrocarbons.

Manufactured in the USA

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391