75 Durometer Fluoroelastomer (FKM) Rubber Sheet

Proudly manufactured in the USA

Description: VIT-770 is a proprietary compounded FKM elastomer product designed for applications that require up to 350°F  service and good chemical resistance.

VIT-770 is compounded  to offer excellent value for gasket sealing applications

Typical Physical Properties

| Durometer (Shore A) Hardness | 75+/-5 |
| --- | --- |
| Tensile Strength (psi) | 1200 |
| Elongation | 225% |
| Temperature Rating (operating) | -20(F to +350(F |
| Color | Black |
| Specific Gravity | 1.76 |
| Finish | Smooth with light talc |

Physical Properties shown were obtained on a molded .080” ASTM Sample.   These are typical results.

Stigall Style: VIT-770 is a low cost alternative for applications that do not require the heat resistance of 100% Fluoroelastomer.  It is the customers responsibility to qualify this product for its fitness for use.  This product is NOT recommended for mineral acids, ketones, low molecular weight esters or nitro hydrocarbons.

Manufactured in the USA

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391